## Slide 1: X-ray diffraction at extreme conditions: tools and practice
Introduction

## Slide 2: Extreme conditions?
An extreme environment contains conditions that are hard to survive for most known life forms (Wikipedia.org)
..research in nuclear physics relates to the study of nuclei under extreme conditions such as high spin and excitation energy.. (Wikipedia.org)

## Slide 3: Extreme conditions
Extreme conditions are conditions expanding the current thermodynamic state beyond the limits of the ambient.
P-V-T-H-E-t-.. phase diagram
P | Pressure
V | Volume
T | Temperature
H | Magnetic Field
E | Electrical Field
t | Time

## Slide 4: Extreme high pressure P-V-T-t
specific states of matter
phase equilibria
fundamental materials
applied materials

## Slide 5: Extreme high pressure P-V-T-t
P-T (no chemistry):
clean adjustment
no doping
P-T (chemistry):
new bonding
new materials

## Slide 6
P-t conditions
dynamic
static

## Slide 7: Field practice

## Slide 8: Know-how..

## Slide 9: Know-how..

## Slide 10: Course outline
Lectures
Understand your experiment
X-ray source
Sample environment
Detectors
Seminars
Understand your pressure
Understand your signal
Preparation for HP experiment:
Calibration
Data simulation
Processing powder
Processing single crystal
Data processing:

## Slide 11: History of the X-rays
1895
W. C. Röntgen
Discovery
of the X-rays
Penetrating radiation
M. von Laue
W. H. Bragg
W. L. Bragg
1912
X-rays as waves produce
interference patterns.
Detected intensities correspond to diffraction
of planes with specific atomic arrangement.
Bragg’s law
X-rays in techniques used for structure determination of small and large molecules; crystalline, amorphous and nano-scale materials (diffraction).
Chemistry characterization (electron and nuclear based spectrometry such as fluorescence and etc.)
Etc. etc. etc.
Braggs law
Images – courtesy of the internet

## Slide 12: EM spectrum + X-rays
courtesy of Advanced Light Source

## Slide 13
Source
Collimation
Focusing
Sample
Detector

## Slide 14: X-rays sources
WTF!?
MoKα?
X-ray Sources and capabilities
In general and for extreme conditions
Oldies
Newbies
Notes: You may find some annoying specimens around
Like the specimens -

## Slide 15: Lab. X-ray sources
1870
Crookes tube from
W. C. Röntgen museum
W. Crookes
‘cold tubes’
1913
1917
W. Coolidge
fixed anode
Notes: William Crookes
Cold emission – DC voltage 100kV cathode -0 right and anode center+left. Low pressure 10-6-10^-8 atm. Gas atom ionized – positive ions – go to the cathode, create more electrons. High speed electron go for anode and produces bremsstrahlung + characteristic lines.
William Coolidge

## Slide 16: Lab. X-ray source: W. Coolidge tube
Cathode
i.e. tungsten
Anode
Materials producing
char. X-rays.
Rhodium target
bremsstrahlung
Characteristic X-rays
Kα1 (20.2keV, 0.61A) Kβ1 (22.7keV, 0.54A)
Notes: The bremsstrahlung or free - free emission mechanism is an example of a radiative process of considerable interest in modern astrophysics. This mechanism involves the emission of a photon by an electron due to an electrostatic interaction with another charged particle. In other words, when an electrons path is deviated by a charged atomic nucleus it can emit or absorb a photon
Compton is a mechanism of scattering

## Slide 17: Lab. X-ray sources
1870
Crookes tube from
W. C. Röntgen museum
W. Crookes
‘cold tubes’
1913
1917
W. Coolidge
fixed anode
1929
Philips produces
First rotating anode
‘Rotalix’
idea or. from 1897
1934
Siemens produces
`Pantix`
Notes: William Crookes
Cold emission – DC voltage 100kV cathode -0 right and anode center+left. Low pressure 10-6-10^-8 atm. Gas atom ionized – positive ions – go to the cathode, create more electrons. High speed electron go for anode and produces bremsstrahlung + characteristic lines.
William Coolidge

## Slide 18: X-ray source: Rotating anode
Tapered
anode
X-rays
Simple tube
Rotating
anode

## Slide 19: Lab. X-ray sources
Liquid metal
sources
Philips produces
First rotating anode
‘Rotalix’
idea or. from 1897
1929
1934
Siemens produces
`Pantix`
2005
Fancy anode
Anode – fixed,
Tube is rotating
Made in Germany
Notes: William Crookes
Cold emission – DC voltage 100kV cathode -0 right and anode center+left. Low pressure 10-6-10^-8 atm. Gas atom ionized – positive ions – go to the cathode, create more electrons. High speed electron go for anode and produces bremsstrahlung + characteristic lines.
William Coolidge

## Slide 20: Lab. X-ray sources: Liquid metal
Kα1: Ga – 9keV (1.35Å); In – 24.2keV (0.51Å);
Notes: William Crookes
Cold emission – DC voltage 100kV cathode -0 right and anode center+left. Low pressure 10-6-10^-8 atm. Gas atom ionized – positive ions – go to the cathode, create more electrons. High speed electron go for anode and produces bremsstrahlung + characteristic lines.
William Coolidge

## Slide 21: Typical wavelengths for laboratory sources: how is it for the HP diffraction?
Source mat. | Wavelength, Å | Energy, keV
Cr | 2.28 | 5.415
Fe | 1.94 | 6.404
Co | 1.79 | 6.93
Cu | 1.54 | 8.048
Ga* | 1.35 | 9.252
Mo | 0.71 | 17.479
Rh | 0.61 | 20.216
Ag | 0.56 | 22.163
In* | 0.51 | 24.209
Au | 0.18 | 68.804
* - liquid metal source
Useful for small HP environments (diamond anvil cell)
Large focus spot – low noise to background ratio (<100µm)
Low flux at high energy
Useless for large HP environments

## Slide 22: Alternative sources: synchrotron radiation X-ray sources
1944-1945
Ivanenko
Pomeranchuk,
USSR
Schwinger US
Calculations on synchrotron radiation
1947
Observation of
synchrotron
radiation
Rapid development of synchrotron radiation facilities
Present – 4th generation of the sources
1962
Present days
Synchrotron radiation is the name given to the radiation which occurs when charged particles moving at relativistic velocities are accelerated in a curved path or orbit, i.e. under influence of magnetic fields
Notes: William Crookes
Cold emission – DC voltage 100kV cathode -0 right and anode center+left. Low pressure 10-6-10^-8 atm. Gas atom ionized – positive ions – go to the cathode, create more electrons. High speed electron go for anode and produces bremsstrahlung + characteristic lines.
William Coolidge
In – 24kEV
Observation of synchrotron radiation – by mistake

## Slide 23: Can we find synchrotron radiation in nature?
?

## Slide 24: Synchrotron light source
Synchrotron radiation is the name given to the radiation which occurs when charged particles moving at relativistic velocities are accelerated in a curved path or orbit, i.e. under influence of magnetic fields
Bending magnet
Bunch of
Electrons/positrons
X-ray radiation
cone
Undulator

## Slide 25: Energy bandwidth and flux of different magnetic structures
Combination of accessible energy range,
selectable energy bandwidth,
high flux and brilliance
make synchrotron sources
extremely attractive for high pressure research
Notes: That is why most of the modern large scale synchrotron facilities have high pressure beamlines

## Slide 26: Time factor – pump and probe experiments
Electrons travel as bunches.
Typical Petra-III modes:
40
60
240
480
960
Single bunch is a charge carrying
electronic cloud
Bunches are separated by time
Bunches travel with relativistic velocity through
a complex magnetic array
Time separation between bunches can be used
for timing experiments:
Pump/Probe
Pump/Probe/Probe/Probe

## Slide 27: Future
X-ray lasers

## Slide 28: Future
Swiss Light source
tiny e-beam
accelerator
Huge accelerator
Lost of magnetic structures
SACLA – RIKEN
Japan

## Slide 29: Accessible energy bandwidth
A. Di Piazza et al. Rev.Mod.Phys. 84 (2012)
European XFEL
Largest X-ray free electron laser
27kHz repetition rate
0.05 to 4.7Å
Peak brilliance
5·1033
(photons / s / mm2 / mrad2 / 0,1% bandwidth)
Suitable for high pressure research

## Slide 30: Extreme timescale resolution of XFELs

## Slide 31
Extreme challenges of XFELs
Small angle X-ray diffraction

## Slide 32: Things to take away
X-ray sources for high pressure
Lab. sources
  Useful for compact environments (DACs)
  Useless for large scale environments
Large scale sources
  Useful for both: compact and large high pressure environments
  Additionally offer data collection with enhanced time resolution

## Slide 33: Things to take away
  Important info for the source
Energy
Energy bandwidth
Brilliance
Emittance
Size
Repetition rate
Damage threshold