## Slide 1: X-ray diffraction at extreme conditions: tools and practice
Signal from a DAC – monochromatic X-rays

## Slide 2
Maximal opening of the cell:
2θ≤40-45o

## Slide 3
Structure
Volume
Phase diagrams

## Slide 4: Things to consider for your experiment
Material
Lattice (crystallographic info)
Ranges for 2θ, d-space, Q-range
Peak overlap
Chemistry (Z; scattering, vol.)
Instrument
Energy (2θ range for given opening)
DAC
Maximum pressure
Geometry of collection
Opening angle
X-ray beam size on sample
Pressure medium
Size of the detector
Detector – sample distance
Efficiency of the detector (energy)
Powder or single crystal?

## Slide 5: Material – powder vs single crystal - cheatsheet
For a given Z and sample volume:
Single crystal scatters stronger in a diffraction direction
Single crystal is free from intergrain interactions, microstrains (diffraction lines are thinner); gain in peak resolution
Single crystal signal is free from effects of preferred orientation on diffraction intensities
Better treatment of close peaks (treating overlapping intensities in powder)
Single crystal signal is more reliable than powder for structure determination
One can treat single crystal signal as powder (1D integration)
Still image or small oscillation
Want data?
Rotate!!!

## Slide 6: Material – powder vs single crystal - cheatsheet
But:
good single crystals are harder to get; especially for layered structures
Even the best of the crystals does not guarantee successful data solution for a compression induced transition into a new phase (twinning, strain, etc.)
Sometimes refinement of powder data can indeed shed light on the structure (submicron grain size, no preferred orientation, special atomic positions in crystal structure, etc.) Think of reproducibility!
Still image or small oscillation
Want data?
Rotate!!!

## Slide 7: Good data set for structure refinement
Useful data set
As complete as possible
(orientation, DAC opening, energy)
Maximum resolution achievable
(high 2θ, cell opening)
As less systematic errors as possible:
Overlapping (in 2θ – detector pixel size; beam divergence)
Good crystal
Detector overload
Radiation damage

## Slide 8
What is a good crystal
?

## Slide 9: Good data set for lattice parameters
Useful data set
As better signal/noise ration at high 2θ as possible
As less systematic errors as possible:
Monochromatic, non divergent beam
Good crystal / fine powder
Rotation of the cell (sample); s.c. - 8 - position centering
Point detector is better than 2D detector (pixel size as limiting factor)

## Slide 10: Resolution of diffraction data
Total number of unique data
High 2θ - better
Amount of information
Structural solution
Powder still image
Higher resolution – more accurate information on the atomic positions
Low resolution
High resolution
proteinstructures.com

## Slide 11: Resolution of diffraction data
Total number of unique data
High 2θ - better
Amount of information
Structural solution
Powder still image
Low resolution
High resolution
Low resolution
High resolution

## Slide 12: Resolution of diffraction data
Total number of unique data
High 2θ - better
Amount of information
Hunting for intensity at high 2θ we sacrifice resolution of diffraction peaks – accuracy of lattice parameters determination
Structural solution
Lattice parameters – peak shape
Intensity is registered as a peak with certain shape
Peak shape of the registered beam is convolution:
–energy bandwidth
–beam divergence
–detector acceptance
–grain size
–strain
Powder still image

## Slide 13
Increase volume
Use lower energies
Low Z materials
Lower energies – more flux

## Slide 14: Remember about environment
X-ray
Especially important for powders

## Slide 15: Remember about environment
X-ray

## Slide 16: Real world situation

## Slide 17: Hydrostatic compression

## Slide 18: Powder+Single crystal data
Data collection
Masking + Integration
Indexing (phase-peak)
Volume determination
Structure solution
Bragg’s law

## Slide 19: Pressure – Volume (a,b,c) as elastic property
 | Volume at ambient pressure
 | Compressibility
 | Bulk modulus at ambient pressure
 | Bulk modulus at ambient pressure
 | Bulk Modulus derivatives at ambient pressure
 | Volume at ambient pressure
 | Compressibility
 | Bulk modulus at ambient pressure
 | Bulk modulus at ambient pressure
 | Bulk Modulus derivatives at ambient pressure
Equations of states relate volume, pressure and elastic moduli

## Slide 20: Pressure – Volume (a,b,c) as elastic property - EOS
There is no absolute thermodynamic basis for specifying a correct form for an EoS (all based on assumptions)
All EoS – stress / strain relations
Practical EoS:
assumed interatomic potentials
assumed relationship between P and EoS parameters (finite strain)
assumed relationship between free energy and strain (natural strain)
after Ross Angel

## Slide 21: Vinet EOS – interatomic potential
after Ross Angel
 | Energy is a function of interatomic distances (r0, r)
 | Definition of strain
 | 3 parameter equation relating pressure and volume
 | K’’ is fixed
 | Energy is a function of interatomic distances (r0, r)
 | Definition of strain
 | 3 parameter equation relating pressure and volume
 | K’’ is fixed
Good for simple solids
Accurate to high compression
Not intended for materials with significant internal freedom
EoS order is fixed by the equation

## Slide 22: Birch-Murnaghan EoS – finite strain EoS
after Ross Angel
Expansion of conventional elasticity (infinitesimal strains) to substantial strains
 | strain energy (E) as a polynomial function of strain (f)
 | Definition of Eulerian strain (final state)
 | strain energy (E) as a polynomial function of strain (f)
 | Definition of Eulerian strain (final state)

## Slide 23: Birch-Murnaghan EoS – finite strain EoS
after Ross Angel
Expansion of conventional elasticity (infinitesimal strains) to substantial strains
2nd/3rd order
Fits P/V to V/V0 ~0.8
Provides correct K0
Cannot be inverted

## Slide 24: Birch-Murnaghan EoS – finite strain EoS – second order
after Ross Angel
Large variety of materials have K` close or equal to 4
If it is strongly deviated – warning sign

## Slide 25: F-f plots and BM EoS – tool to check your EoS
after Ross Angel
Normalized Stress as a function of Eulerian strain (fE):
Be careful with higher orders

## Slide 26: F-f plots as a tool to detect phase transition
Detection of isostructural transition.
Electronic spin state transition of Fe2+ manifested in volume contraction

## Slide 27: Natural strain EoS (Poirier)
after Ross Angel
 | Definition of Natural strain
 | Definition of Natural strain
Assumed relation between free energy and strain
Not very convenient
Almost not used in community

## Slide 28: Structure solution
First group
Purely geometrical modelling
Finding analogous
Examining packing
Using minimization methods
Energy
Second group
Using structural amplitudes for initial model – work in the reciprocal space
Entropy
Geometrical constraints
Patterson (`heavy atom`) technique
Direct phase technique

## Slide 29: X-ray diffraction phase problem
Structure amplitude (Unit cell):
Electronic density in Fourier transform:
phase - cannot
be measured
directly!!!
obs.
intensity
Pecharsky and Zavalij (2005)

## Slide 30: Patterson function
Electronic density in Fourier transform:
Patterson function (synthetic) represents distribution of interatomic vectors:
Patterson function is a self convolution of electronic density:
Pecharsky and Zavalij (2005)

## Slide 31: Patterson function
Electronic density in Fourier transform:
Patterson map:
Map contains peaks, which are related to the real distribution of atoms in the u.c.
it is possible to establish both the coordinates of atoms and their scattering power by analyzing coordinates and heights of Patterson peaks.
peaks begin from a common point: origin of the unit cell.
Pecharsky and Zavalij (2005)

## Slide 32: Patterson function
Complications:
peaks; n – total number of atoms
Patterson peaks are broader (convolution effect)
Overlapping of the vectors for large number of atoms
Limited usefulness for large lattices with many atoms of similar Z (i.e. organic)
Very useful for small lattices
Starting position for heavy Z atoms (electronic density squared)
Pecharsky and Zavalij (2005)
Arthur Lindo
Patterson

## Slide 33: Direct methods – try to recover phase from intensities
These properties establish certain phase relations between hkl triplets (depending on atomic scattering factor):
h,k, l
h’,k’, l’
h-h’, k-k’,l-l’
Electronic density is non negative everywhere in the cell
Atomic structure – spherical atoms
Observed structure amplitudes are scaled and normalized
Several strong intensities (triplets) are used for phase permutations
Phases are assigned to as many as possible reflections and then a least square algorithm is used for refinement to cover the rest
Electronic density map is calculated and judged (crystallographic and common sense)
Pecharsky and Zavalij (2005)

## Slide 34: Structure solution – remember about environment
H.P. Environment – provides intensities overlapping with your data:
diamond, pressure medium, gasket, pressure sensor, etc.
Physical limit of the detector – oversaturation of the intensities
Filter your data in smart way
Notes: Add here a description of the data - sample loses intensity because the first diamond is reflecting a part of it.

## Slide 35: Structure solution – remember about environment
Pressure medium or environment can penetrate your material
Expect change of chemistry for your material, additional peaks in electronic map

## Slide 36: Effects of Non-Hydrostatic compression
=

## Slide 37: Effects of Non-Hydrostatic compression
Geometry of compression
Stress-strain:
=

## Slide 38: Effects of Non-Hydrostatic compression
Non hydrostatic effects arise.
Macro level:
Geometry of compression
Redistribution of pressure inside sample chamber
Micro level:
Intergrain interactions
Preferred orientation
Geometry of compression
Stress-strain:
=
after Singh (1997)

## Slide 39: Geometry of compression

## Slide 40: Geometry of compression – deviatoric stress
Mean stress
Uniaxial component
Deviatoric stress
-
after Singh (2004)

## Slide 41: Geometry of compression – deviatoric stress
You may have deviatoric stress even at quasihydrostatic conditions
This stress leads to an effect of pressure overestimation
Consider P1=P2
If you have deviatoric stress and volume V
and non zero value of t

## Slide 42: Geometry of compression – deviatoric stress
Smaller volume for given pressure– better
Diamond Raman tends
to overestimate pressure

## Slide 43: F-f plots as marker for deviatoric stress
Normalized Stress as a function of Eulerian strain (fE):
Similar materials!

## Slide 44: Take away
Think of reproducibility
Be vigiliant

## Slide 45: Effects of undesirable stresses on diffraction pattern
Shift of diffraction lines f(hkl,θ)
Deviatoric stress
Diffraction line broadening (hkl)
Instrumental function
Particle size
Micro strains (grain-grain interaction)
- Line shift
n – grains; individual stresses
- stress variances
create additional strain and partially responsible for the line broadening

## Slide 46: Influence of deviatoric stress on line shift
Full strain on individual hkl of a single grain:
– angle between load direction and normal
to hkl plane
Hydrostatic strain:
after Singh (2004)

## Slide 47: Influence of deviatoric stress on line shift
Full strain on individual hkl of a single grain:
Q(hkl) – relates individual crystallographic plane behavior and elastic moduli
Hydrostatic strain:
- shear moduli (Reuss)
- shear moduli (Reuss)
– weight of contribution ()
after Singh (2004)

## Slide 48: Origin of Reuss and Voigt
Stress and strain are unknown and considered as non uniform
Reuss and Voigt – boundary models to estimate effective elastic moduli of rocks in terms of properties of the various constituents (grains of different orientations, different phases, pores, and etc.)
Exact geometry is very hard to measure – any realistic case can be approximated by an interpolation of the upper (Voigt) and lower (Reuss) boundaries
- modulus of ith grain or hkl
- volume fraction of ith grain
Reuss limit:
Voigt limit:

## Slide 49: Influence of deviatoric stress on line shift (cubic system example)
Individual hkl line shift for :
After using many assumptions and relations with other elastic constants one can obtain compliance values and revert to elastic moduli
Stress-strain:
- compliance values
- compliance values
- shear moduli (Reuss)
– weight of contribution
- Bulk modulus
;
after Singh (2004)

## Slide 50: But!!!
Individual lines always shift:
– in UNKNOWN
This has been done reliably only on cubic materials: Mo, Au, NaCl.
Lower symmetries, like hexagonal structured materials, like iron
are not precise (Singh et al [2004]).
Wont’work reliably for multiphase materials, especially with strong contrast between elastic properties and significant line overlap.

## Slide 51: A little more on the geometry - parallel
For a given
the whole line changes homogeneously
Individual hkl line shift:
– angle between load direction and normal
to hkl plane
0o0o
50o90o
circle

## Slide 52: A little more on the geometry - radial
Individual hkl line shift:
– angle between load direction and normal
to hkl plane
ellipse
0o0o
90o

## Slide 53: Diffraction line broadening
Diffraction line broadening (hkl)
Instrumental function
Particle size
Micro strains (grain-grain interaction)
Other effects

## Slide 54: Diffraction line broadening
Compression:
Induces strain between individual grains
Crushes grains and changes their size distribution

## Slide 55: Diffraction line broadening
 | Fullwidth at half maximum of hkl reflection (in )
 | Wavelength
 | Average grain size independent of hkl
 | Micro strain contribution
 | Wavelength
 | Average grain size independent of hkl
 | Micro strain contribution
after Singh (2006)
Effect is orientation sensitive

## Slide 56: Diffraction line broadening
Phase coexistence region
Higher strain in hcp phase
Grain size – always distribution
Grain size – not really precise

## Slide 57: Diffraction line broadening
Small, homogenous grain is a must
Instrumental function is a must
You can try to estimate only an average grain size
Large number of grains is a must
Uniform diffraction rings is a must
You can use this signal for phase transition detection
You can use this signal for sample bridging between diamonds
Precision is not quite there
Less useful for multiphase materials
No add. contributions to the width

## Slide 58
Thank you!