## Slide 1: X-ray diffraction at extreme conditions: tools and practice
Signal from high pressure environment

## Slide 2: Classification of compression experiments
By volume
Small volume
Static compression
By compression rate
Dynamic compression
Based on static compression
Based on shock compression
DAC – dia. anvil cell
Large volume
Paris-Edinburgh press
Drickhamer press
Multi-anvil press
Small volume
DAC – dia. anvil cell

## Slide 3: X-rays and interaction with matter
Absorption
Scattering on electons

## Slide 4: Thomson scattering – by an e-

## Slide 5: Thomson scattering – by an e-
Differential crossection:
P – polarization factor
r0 – Thomson scattering length (electron)
Polarization | Description
 | synchrotron vertical scattering
 | synchrotron horizontal scattering
 | unpolarized source
Polarization | Description
 | synchrotron vertical scattering
 | synchrotron horizontal scattering
 | unpolarized source

## Slide 6: Growing in scale: atom
Atom has many electrons – phase shift occurring for electrons for scattering angle ≥0
Q – wave vector transfer or scattering vector
This results in minor interference for different scattering angles
Total scattering of the atom:
– electron density for a volume unit
– atomic form factor

## Slide 7: Growing in scale: atom
Electrons are quantum bodies with specific energies in an atom K, L, M, etc.
Dispersion corrections to are introduced
Efficiency of scattering drops if incoming energy is smaller then, for example K edge energy (correction for bound electron):
Existence of K,L,M edges and resonant absorption corresponds to another term

## Slide 8: Growing in scale: atom
Wikipedia.org
O
Cl
Cl-
K+

## Slide 9: Growing in scale: crystal
Crystal has atoms arranged in a periodic fashion (long range order)
Bragg’s law:
Crystal structure factor:
unit cell
structure
factor
lattice sum

## Slide 10: Growing in scale: crystal
Crystal structure factor:
Reciprocal space and Direct space:
Scattering from a crystal is therefore confined to distinct points in reciprocal space

## Slide 11: Growing in scale: crystal – monochromatic X-ray

## Slide 12: Growing in scale: crystal – polychromatic X-ray

## Slide 13: Magnetic interactions
An X-ray photon can interact with electron.
Can this photon interact with its spin and orbital moment?
Short answer: yes, but.
Interactions with spin-orbit degrees of freedom are much weaker
Only small fraction of electrons have order in spin/orbital moments
Contribution to the intensity is 10-6 smaller
Challenging, but can be done for antiferromagnetic structures, at resonant energies (!!! – low energies)
Challenging, but can be done at high pressures (Ir, large Z)

## Slide 14: X-ray signal

## Slide 15: X-ray signal: Compton scattering
Compton scattering induces variation of X-ray photon energy:
Compton scattering produces smooth background for any material:
Gas
Liquid
Solid
Compton scattering length:

## Slide 16: X-ray signal: Compton scattering
For XRD – background signal

## Slide 17: X-ray signal

## Slide 18: X-ray signal: photo electrons & fluorescence
XRD?
fine.
XRD?
Produces background

## Slide 19: Absorption
Change of incoming X-ray intensity with thickness:
Single element material:
Multi element material:
 | Absorption coefficient
 | Atomic number density
 | Absorption crossection
 | Mass density
 | Avogadro number
 | Mass
 | Absorption coefficient
 | Atomic number density
 | Absorption crossection
 | Mass density
 | Avogadro number
 | Mass

## Slide 20: X-ray diffraction and HP environments
Environment affects
Absorption (lowers amount of X-rays on your sample)
Scattering (adds to incoherent; background Compton)
Fluorescence yield (background; lower signal/noise)
Scattering (adds to coherent; additional peaks)
Absorption (absorbs signal from the sample; lower signal/noise)

## Slide 21: X-ray diffraction and HP environments
Environment is a complication

## Slide 22: X-ray diffraction and HP environments
Environment is a complication
X-ray

## Slide 23: X-ray diffraction and HP environments
Absorption by environment
Absorption by sample

## Slide 24: Examples: DAC
Thick diamond reflects considerable amount of intensity.
This intensity can become a source for secondary diffraction (gasket). Bad for powder and amorphous material data.
still image

## Slide 25: Examples: Multianvil
Signal from
the sample

## Slide 26: How to fight undesirable signal?
Soller slits: sacrifice signal,
improve signal/noise ratio
Gaussian form of the beam
reduce tails
Smaller, less divergent beam:
higher signal/background

## Slide 27: Useful X-ray scattering signal

## Slide 29: X-ray diffraction on crystalline solids
hkl
Real and reciprocal space
x,y,z – coordinates of atoms in the unit cell
hkl – indexing of lattice planes with
the specific dhkl –spacing in the
reciprocal space
Bragg’s law

## Slide 30: Powder vs Single crystal
Powder still image
Single crystal precession image
Always some orientation for diffraction
Want diffraction?
Rotate!!!

## Slide 31: Intensity from X-ray diffraction on crystalline solids
after Pecharsky and Zavalij (2005)
Fundamentals of powder diffraction
 | Diffracted intensity | Powder | Single crystal
 | Scale factor (unit cell vs full crystal) | x | x
 | multiplicity factor – multiple symmetrically equivalent positions (100, 010 and 001 for cubic system) | x | 1
 | Lorentz factor – geometry of collection | x | x
 | Polarization factor | x | x
 | Absorption factor – absorption of the incident and diffracted beams | x | x
 | Preferred orientation factor | x | 1
 | Extinction factor – deviation from kinematic model | 1 | x
 | Structure factor or diffracted amplitude (atomic positions) | x | x
 | Diffracted intensity | Powder | Single crystal
 | Scale factor (unit cell vs full crystal) | x | x
 | multiplicity factor – multiple symmetrically equivalent positions (100, 010 and 001 for cubic system) | x | 1
 | Lorentz factor – geometry of collection | x | x
 | Polarization factor | x | x
 | Absorption factor – absorption of the incident and diffracted beams | x | x
 | Preferred orientation factor | x | 1
 | Extinction factor – deviation from kinematic model | 1 | x
 | Structure factor or diffracted amplitude (atomic positions) | x | x

## Slide 32: Scale factor: Powder vs Single crystal for High Pressure
Advantage powder:
Single shot – many hkls
Advantage single crystal:
Same material volume, single crystal scatters better – higher signal/noise ratio
Same volume:
A grain of powder has less unit cells than single crystal

## Slide 33: Intensity multipliers - Lorentz factor
- Lorentz factor – geometry of collection
after Pecharsky and Zavalij (2005)
Fundamentals of powder diffraction
Mult. factors | 
 | Finite size of reciprocal space
 | Geometry of collection (receiving slit) The number of crystals oriented in such a way as to satisfy Bragg’s Law is highest for low angles The fraction of the diffraction cone that intersects the detector is highest at low angles
 | s.c. – different hkls do not have the same time of passing through the Bragg condition ~time permitted for each reflection ~1/velocity for plane to pass through reflection
Mult. factors | 
 | Finite size of reciprocal space
 | Geometry of collection (receiving slit) The number of crystals oriented in such a way as to satisfy Bragg’s Law is highest for low angles The fraction of the diffraction cone that intersects the detector is highest at low angles
hkl

## Slide 34: Intensity multipliers - Lorentz factor

## Slide 35: Preferred orientation ; only powders
Preferred orientation affects intensity relation of individual diffraction peaks – suppresses ones, increases the others

## Slide 36: Preferred orientation ; only powders
At high pressure PO may evolve (uniaxial compression, DAC, small volume)
Thus, should never be considered constant or known for small volume high pressure experiment
Attention – extreme care with structure solution for data based on powders!!!
starting material
pressurized material

## Slide 37: Extinction factor - mostly for single crystals
– function of shape, structure amplitude and number of unit cells per volume

## Slide 38: Structure factor - structure contribution
 | Structure factor
 | Population, occupancy of an atomic position
 | Temperature factor (Atomic Displacement Parameters - ADPs)
 | Atomic scattering factor (, Z)
 | – scalar product of coordinates with HKL
 | Structure factor
 | Population, occupancy of an atomic position
 | Temperature factor (Atomic Displacement Parameters - ADPs)

## Slide 39: Thermal parameters: isotropic approximation
-isotropic displacement parameter for jth atom
- root mean square deviation of jth atom from its (xj, yj, zj)

## Slide 40: Thermal parameters

## Slide 41: Take away:
  Important info for the signal
Scattering from electron to crystal lattice – how it works
Different types of signal: useful and not (emphasize on environment and background)
Diffraction as scattering: common and different features of single crystal and powder.
Diffracted intensity carries information: geometry, chemistry, structure
Be extremely careful with using powder for structure solution