## Slide 1: X-ray diffraction at extreme conditions: tools and practice
High pressure environments

## Slide 2
H
P
igh
ressure

## Slide 3: Extreme high pressure P-V-T-t
specific states of matter
phase equilibria
fundamental materials
applied materials

## Slide 4: Classification of compression experiments
By volume
Small volume
Static compression
By compression rate
Dynamic compression
Based on static compression
Based on shock compression
DAC – dia. anvil cell
Large volume
Paris-Edinburgh press
Drickhamer press
Multi-anvil press
Small volume
DAC – dia. anvil cell

## Slide 5: Compression

## Slide 6: Compression

## Slide 7: Compression

## Slide 8: Compression

## Slide 9: Compression

## Slide 10: Compression

## Slide 11: Compression

## Slide 12: Compact environments – diamond anvil cell

## Slide 13: Compact environments – diamond anvil cell
sliding
surface
Pressurized cell
Open cell
BGI design

## Slide 14: Compact environments – diamond anvil cell
sliding
surface
Pressurized cell
Open cell
Lawrence-Livermore design

## Slide 15
How many screws does a student need to pressurize a DAC?
How many screws does a professor need to pressurize a DAC?

## Slide 16: X-ray diffraction in a DAC
X-rays perpendicular to compression
X-rays uniaxial with compression
Force is applied along a certain axis
Strongly non-hydrostatic conditions
Quasi-hydrostatic conditions

## Slide 17: X-ray diffraction in a DAC
Limiting factor:
Opening of the cells
In reality you should think in d-spacing or Q range coverage (Bragg law)
Energy is important!!!
For monochromatic beam
42keV ; λ=0.29 Å
2θ≈25o – powder
2θ≥28o – single crystal
optimal - 35o
Mao-type cell

## Slide 18: Large volume press (Drickhamer)
Balchan & Drickhamer (1961)
Relatively small press
Can generate over 30 Gpa with
Sample about 0.2-0.3 mm in linear dimension
after Y. Wang (2010)
White beam & monochromatic beam

## Slide 19: Large volume press (Paris-Edinburg)
Hydraulic compact press with almost spherical sample chamber (≤1mm3)
up to 20-30GPa with sintered diamond anvils and high temperature (2000K)
after G. Shen (2014)
White beam &
monochromatic beam
Anvil

## Slide 20: Large volume press (Multianvil)
Highest pressure depends on assembly (smallest volume)
and anvil material
White beam & monochromatic beam
after Y. Wang (2010)
Octahedron as complex sample chamber
Synthesis, stress-strain relations, most versatile in D-DIA modification
WC or
synt. diamond
anvil

## Slide 21: X-ray data collection schemes

## Slide 22: Source properties
White beam
Monochromatic
beam
Braggs law: ; Energy:
Monochromatic X-rays: Si (111)
E=40keV – =4-8eV

## Slide 23: Detection principle
Ge or Si
based
White beam
Monochromatic
beam

## Slide 24: Detection principle – with point detector
Ge or Si
based
Can be used in energy dispersive mode:
White X-ray beam
Fixed 2θ angle
Can be used in monochromatic mode:
Monochromatic beam
Scanning 2θ angle or any other angle
Signal accuracy or resolution is controlled
Source size+Energy
Distance
Angular step size
Slit opening
slits

## Slide 25: Detection principle – with 1D/2D detector arrays
Slowly replace point detectors for monochromatic applications
Area collection is faster then point by point collection
2D signal collection + higher and higher detection efficiency
Resolution is controlled by:
  Energy+Focusing
  Distance
  Pixel size
Image plate, CCD, Flat panel,
CMOS single photon counting panels

## Slide 26: Detection principle
What is better:
Area detector
Point detector
?

## Slide 27: Typical DAC experiment (monochromatic beam)

## Slide 28: Typical Multi-Anvil experiment (white beam)
after Wang (2010)

## Slide 29: Typical Multi-Anvil experiment
SPEED-1500, a 6/8 system at SPring-8 (Spring-8 website)

## Slide 30: Typical Multi-Anvil experiment
X-ray
38ton - 20 MN (Voggenreiter site)
similar to one installed at ID06 (ESRF)

## Slide 31: Shock compression environments
Maximal available pressure on iron during underground nuclear tests
Stationary shock wave:
Shock with
2-6x10-60mm

## Slide 32: Shock compression environments
Light gas guns
Fire projectile, hit target, create shock

## Slide 33: Shock compression environments
in vacuum

## Slide 34: Shock compression environments
Usage of X-ray free electron laser is a must for such studies:
extreme time resolution, extreme pulse intensity
High temperature is a by product of shock compression.
VISAR records reflectivity change on a back of a target as a function of time
Detects shock propagation time